Figure S1. Long-term operational stability and the Faradaic efficiency of the flow cell.

Table S1. Comparison of electrochemical H2O2 generation systems with reported literature.

| Cathode /Catalyst | pH | Current density (mA cm-2) | Time (h) | O2 flow rate (L min-1) | H2O2 production rate (mg h-1 cm-2) | References |
| --- | --- | --- | --- | --- | --- | --- |
| 39BB carbon paper | 1.2-1.5 | 200 | 0.67 | 0.02 | 116.8 | This work |
| Dual rotating graphite felt | 3 | 50 | 1 | 0 | 0.58 | Environ. Sci. Technol. Lett. Vol. 1, pg. 320-324, 2014 |
| CNT-PTFE cathode | 3 | 204 | 5 | 0.14 | 12.8 | Electrochim. Acta. Vol. 54, pg. 6651-6660, 2009 |
| Acetylene black-PTFE cathode | 3 | 120 | 2.5 | 0.41 | 12.8 | Electrochim. Acta. Vol. 56, pg. 8651-8656, 2011 |
| Modified graphite felt | 3 | 50 | 1 | 0 | 22.1 | Electrochim. Acta. Vol. 163, pg. 182-189, 2015 |